## Slide 1: Fittings
Francis Adoah

## Slide 2
Project 1: HATNA derivatives with electron-donating/withdrawing groups
F4-HATNA-OC10SAc
(MeO)4-HATNA-OC10SAc
(NO2)4-HATNA-OC10SAc
(NH2)4-HATNA-OC10SAc

## Slide 3
Molecule |  |  | Energy levels (eV) |  |  |  |  | Surface coverage (10-10 mol/cm2) c
 |  | EHOMO | ELUMO | ELUMO+1 | ELUMO+2 | EFa | Egapb | 
HATNA | Exp. | -6.33d | -3.52d | -3.30d | -2.97d |  | 2.81 | 2.73±0.35
 |  | -6.90e | -4.09e |  |  |  |  | 
 |  | -6.28f | -3.47f |  |  | 4.18 |  | 
 | Theor.g | -6.17 | -2.79 | -2.37 | -2.31 |  |  | 
F4-HATNA | Exp. | -6.41 | -3.62 | -3.26 | -2.96 |  | 2.79 | 1.32±0.14
 |  | -6.89 | -4.10 |  |  |  |  | 
 |  | -6.12 | -3.33 |  |  | 4.02 |  | 
 | Theor. | -6.37 | -3.09 | -2.67 | -2.62 |  |  | 
(MeO)4-HATNA | Exp. | -6.18 | -3.44 | -3.16 | -2.74 |  | 2.74 | 2.96±0.19
 |  | -6.83 | -4.09 |  |  |  |  | 
 |  | -5.80 | -3.06 |  |  | 3.88 |  | 
 | Theor. | -5.99 | -2.58 | -2.2 | -2.11 |  |  | 
(NO2)4-HATNA | Exp. | -6.75 | -4.15 | -3.89 | -3.58 |  | 2.60 | 2.33±0.13
 |  | -6.71 | -4.11 |  |  |  |  | 
 |  | -6.83 | -4.23 |  |  | 3.76 |  | 
 | Theor. | -6.65 | -4.11 | -3.71 | -3.62 |  |  | 
(NH2)4-HATNA | Exp. | -5.65 | -3.37 | -2.79 | -2.64 |  | 2.28 | 2.00±0.10
 |  | -6.39 | -4.11 |  |  |  |  | 
 |  | -5.41 | -3.13 |  |  | 4.01 |  | 
 | Theor. | -5.45 | -2.23 | -1.81 | -1.74 |  |  | 
H6-HATNA | Theor. | -4.35 | -0.38 | -0.34 | -0.27 |  |  | 
F4-(H6-HATNA) | Theor. | -4.68 | -0.77 | -0.68 | -0.66 |  |  | 
(MeO)4-(H6-HATNA) | Theor. | -4.29 | -0.33 | -0.27 | -0.23 |  |  | 
(NO2)4-(H6-HATNA) | Theor. | -5.50 | -3.07 | -3.03 | -2.34 |  |  | 
(NH2)4-(H6-HATNA) | Theor. | -4.00 | -0.05 | 0.05 | 0.10 |  |  | 
Table 1. Summary of surface characterization of HATNA molecules on Au
a Measured with UPS.
b Measured with UV.
c Measured with SAM CV.
d Measured with solution CV and UV.
e Measured with SAM CV and UV
f Measured with UPS and UV.
g Calculated with DFT in gas phase

## Slide 4
HATNA-OC10SAc
TAP-OC10SAc
DAP-OC10SAc
Project 2: HATNA, TAP and DAP derivatives

## Slide 5
Molecule |  | Energy levels (eV) |  |  |  |  |  | Surface coverage (10-10 mol/cm2)c
 |  | EHOMO | ELUMO | ELUMO+1 | ELUMO+2 | EFa | Egapb | 
HATNA | Exp.d | -6.28±0.1 | -3.54 |  |  | -4.18 | 2.74 | 2.73±0.35
 | Theor.e | -6.27 | -2.79 | -2.39 | -2.32 |  |  | 
TAP | Exp. | -6.17±0.1 | -3.43 |  |  | -4.06 | 2.74 | 2.10±0.34
 | Theor. | -6.19 | -2.56 | -2.55 |  |  |  | 
DAP | Exp. | -6.06±0.1 | -3.24 |  |  | -4.16 | 2.82 | 2.86±0.14
 | Theor. | -5.95 | -2.56 |  |  |  |  | 
HATNA-H6 | Theor. | -4.37 | -0.57 | -0.40 | -0.36 |  |  | 
HATNA-H4 | Theor. | -4.24 | -2.38 | -0.67 | -0.59 |  |  | 
HATNA-H2 | Theor. | -4.53 | -2.48 | -2.41 | -0.78 |  |  | 
TAP-H4 | Theor. | -4.36 | -0.57 | -0.31 |  |  |  | 
TAP-H2 | Theor. | -4.48 | -2.48 | -0.65 |  |  |  | 
DAP-H2 | Theor. | -4.31 | -0.57 |  |  |  |  | 
Table 2. Summary of surface characterization of DAP, TAP and HATNA SAMs on Au
a Measured with UPS.
b Measured with UV.
c Measured with CV.
d Measured with UPS and UV.
e Calculated with DFT in gas phase

## Slide 6: Sanity check on (NH2)4-HATNA
SR_data on log-scale
Neg-bias data

## Slide 7: Sanity check on (NH2)4
Neg_bias without log-scale
SR_data

## Slide 8: Sanity check on DAP
SR_data on log-scale
Neg_bias data

## Slide 9: Sanity check on DAP
Neg_bias without log-scale
SR_data

## Slide 10: Scan rate fittings for (NH2)4 & (NO2)4(Project_1)
NO2
NH2

## Slide 11: (NO2)4 parameters

## Slide 15: (NH2)4 Parameters

## Slide 19: Scan rate fittings for F4 & MeO(Project_1)
F4-HATNA
MeO

## Slide 20: F4-HATNA parameters

## Slide 24: MeO-HATNA parameters

## Slide 28: Energy gap comparison

## Slide 29: Scan rate fittings for DAP & TAP(Project_2)
TAP
DAP

## Slide 30: Scan rate parameters for DAP(Project_2)

## Slide 34: Scan rate parameters for TAP(Project_2)

## Slide 38: Energy gap Comparison

## Slide 39: Neg-bias fittings for (NO2)4 & (NH2)4(Project_1)
(NO2)4
(NH2)4

## Slide 40: (NO2)4 Parameters

## Slide 44: (NH2)4 Parameters

## Slide 48: Neg-bias fittings for F4 & MeO(Project_1)
F4-HATNA
MeO-HATNA

## Slide 49: F4-Parameters

## Slide 53: MeO Parameters

## Slide 57: Neg-bias fittings for TAP & DAP(Project_2)
TAP
DAP

## Slide 58: TAP parameters

## Slide 62: DAP Parameters